## Slide 1
1) Wafer Cleaning (RCA 1,2,3)
Oxidizing – Field Oxide (~330 nm)
2) Lithography 1 – Open Source and Drain
Oxide Etch
P - implantation (33 keV; 2E14 cm-2)
3) Lithography 2 – Remove field oxide from the Gate
Oxide Etch (BOE: ~700Å/min)
Gate Oxidation (~20 nm)
4) Lithography 3 – Remove gate oxide from Source and Drain
Oxide etch
Lithography 4 – Create Contacts for Source, Drain and Gate,
Metallization (Al – 110 nm)
Lift Off
5) Characterization

## Slide 2
1-0-0 p-Si
1-0-0 p-Si wafer
We will sink the wafers in a -RCA1 bath (H2O2+NH4OH+H2O2)
-RCA2 bath (2% HF)
-RCA3 bath (H2O2+HCl+H2O2)
Cleaning Process

## Slide 3
1-0-0 p-Si
1-0-0 p-Si wafer
We need to grow a field oxide on the Si surface. We will oxidize (wet) the wafer at 1150 ˚C for 18 min.
We expect to get an oxide thickness of 330 nm .
After the oxidation we will measure the oxide thickness by Ellipsometer

## Slide 4
1-0-0 p-Si
1-0-0 p-Si wafer
We will spinn (4500 rpm, 1 min) a positive photoresist (microposit 1805) on the oxide surface.
After the spinning the wafer will be softbaked at 110 ˚C for 1 minute 20 sec on the hotplate.
Lithography 1- Open Source and Drain
We will load the wafer in the
maskless lithography maskin and
expose the photoresist.
After the exposure we will sink the wafer
into a developer bath for about 1min.
Inspection-Hardbake 120 ˚C for 3 min.

## Slide 5
1-0-0 p-Si
1-0-0 p-Si wafer
We will sink the wafer into a Buffrad Oxide Etch bath (BOE). Etch rate 70 nm/min.
Source and Drain etching

## Slide 6
1-0-0 p-Si
1-0-0 p-Si wafer
P – ions implantation
S
D
Implantation energy is 33 keV and the dose is 2E14cm-2.

## Slide 7
1-0-0 p-Si
1-0-0 p-Si wafer
Lithography 2 – Remove field oxide from the Gate
S
D
We will spinn (4500 rpm, 1 min) positive photoresist on the oxide surface.
After the spinning the wafer will be softbaked at 110 ˚C for 1 minute 20 sec on the hotplate.
We will load the wafer in the
maskless lithography maskin and
expose the photoresist.
After the exposure we will sink the wafer
into a developer bath .
Inspection-Hardbake 120 ˚C for 3 min.

## Slide 8
1-0-0 p-Si
1-0-0 p-Si wafer
Oxide Etch
S
D
We will sink the wafer into a Buffrad Oxide Etch bath to etch the oxide.

## Slide 9
1-0-0 p-Si
1-0-0 p-Si wafer
Gate Oxidation
We will remove the photoresist by aceton and piranha solution (H2SO4+H2O2).
We will grow a thin high quality oxide layer on the surface. The expected oxide thickness is 20 nm

## Slide 10
1-0-0 p-Si
1-0-0 p-Si wafer
Lithography 3 – Remove gate oxide from Source and Drain
We will spinn (4500 rpm, 1 min) positive photoresist on the oxide surface.
The wafer will be sotbaked at 110 ˚C for 1 minute 20 sec.
We will load the wafer in the
maskless lithography maskin and
expose the photoresist.
After the exposure we will sink the wafer
into a developer bath .
Inspection-Hardbake 120 ˚C for 3 min.

## Slide 11
1-0-0 p-Si
1-0-0 p-Si wafer
Oxide Etch
We will sink the wafer into a Buffrad Oxide Etch bath.

## Slide 12
1-0-0 p-Si
1-0-0 p-Si wafer
Lithography 4 – Create Contacts for Source, Drain and Gate
We will spinn (4500 rpm, 1 min) positive photoresist 1813 on the oxide surface.
The wafer will be sotbaked at 110 ˚C for 1 minute.
We will load the wafer in the
maskless lithography maskin and
expose the photoresist.
After the exposure we will sink the wafer
into a developer bath .

## Slide 13
1-0-0 p-Si
1-0-0 p-Si wafer
Metallization
We will put the wafers in an e-beam evaporation chamber to deposit Al (110 nm) onto the surface.

## Slide 14
1-0-0 p-Si
1-0-0 p-Si wafer
Lift-Off
We will put the wafers in a aceton bath combined with an ultrasonic bath
to remove the Al layer above the photoresist.
S
D
G
S
D
G