## Slide 1: KJM 3110 Electrochemistry Chapter 6. Electrodes

## Slide 2: Status and outlook
Till now, we have been introduced to electricity, chemistry and thermodynamics, electrochemical cells and their operating modes
  electrolytic cells (electricity to chemical energy)
  galvanic cells (chemical energy to electricity)
The electrode is the most important and unique part of electrochemistry
Now, we will through several chapters look at electrodes and what goes on there in increasing detail and depth
In Ch 6 “Electrodes” we concentrate on the thermodynamics of electrodes, the null, or open circuit, or Nernst voltage.
  Potentiometry, potentiometric sensors
  (We will not yet look at how it looks (atomically) at electrodes or what happens when we start to draw or apply current (kinetics).

## Slide 3: Electrodes
The electrode of interest is called the working electrode (WE)
Potentials of individual electrodes cannot be measured. We can only measure differences
We need as a minimum one other electrode to apply or measure a voltage and pass or measure a current
The other electrode can be called a counter electrode (CE)
ΔE = EWE – ECE
In electrochemistry we often split the counter electrode so as to use 3 electrodes:
  WE Measure current and potential
  RE Reference electrode (reference potential)
  CE Supply current
ΔE = EWE - ERE
U
I
Source or load
WE
RE
CE
U
I
Source or load
WE
CE

## Slide 4: Reference electrodes
The reference electrode provides a stable reference potential, with no current drawn through it.
By defining the potential of one electrode, we can get a consistent system of electrode potentials
The Standard Hydrogen Electrode (SHE) is chosen as the standard reference electrode, to have a standard potential of 0 V.
A more practical reference is the Ag/AgCl electrode
  AgCl(s) + e- ↔ Ag(s) + Cl-(aq)
It has a standard potential vs SHE of +0.22216 V.
These reference electrodes are suitable for aqueous cells only

## Slide 5: Measurement of a WE potential
The potential of a well-defined working electrode vs a well-defined counter electrode with known electrode potential

## Slide 6: E and ΔG: The book dwells at the Cu2+/Cu cell…

## Slide 7: Standard electrode potentials

## Slide 8: Play with G’s, not E’s…

## Slide 9: The Nernst equation
For a cathodic (reduction) reaction
the half cell potential, defined as the potential of the reactant side vs the product side, is
Reaction quotient Q

## Slide 10: The Nernst equation for cathodic vs anodic reaction
Cathodic (reduction):
Cu2+ + 2e- = Cu
The voltage is that of the product side vs the reactant side:
Eel = Ered = E0red – RT/nF ln(1/[Cu2+]) = 0.34 V - RT/nF ln(1/[Cu2+])
A higher [Cu2+] adds a smaller negative number, hence increases Eel
Anodic (oxidation):
Cu = Cu2+ + 2e-
Eox = E0ox – RT/nF ln[Cu2+] = -0.34 V - RT/nF ln[Cu2+]
A higher [Cu2+] adds a bigger negative number, hence increases |E|
But we measure the voltage still on the metal!
Eel = -Eox = -E0ox + RT/nF ln[Cu2+] = -(-0.34) V + RT/nF ln[Cu2+]
When a reaction is written anodically (as an oxidation), while the voltage is still measured as if it was a cathode, the signs reverse in a Nernst equation.

## Slide 11: Check
Where does the Nernst equation come from, in words and equations?
What happens to the Nernst equation in the following cases:
  Standard state
  General state
  Equilibrium
To repeat: What are the values of Q in the three cases?

## Slide 12: Know the 2.303 and the 59 mV ( ≈ 60 mV) of the Nernst equation
lnx = lnx*logx/logx = logx*lnx/logx = logx*ln10/log10 = logx*ln10 = logx*2.303
(R*298.15)/F)*2.303 = 0.059159 V = 59.159 mV

## Slide 13: Simple element and ion(s) redox and dominance diagrams
Ered (V)
(No x axis)

## Slide 14: Pourbaix diagrams for redox containing H+ or OH-

## Slide 15: Pourbaix diagrams for redox containing H+ or OH-
Horizontal lines: Only redox and potential
Vertical lines: Only acid/base (chemistry), example
Diagonal lines: Both

## Slide 16: Check: Pourbaix diagram
Write the reactions for these two lines (without peeking in the book)

## Slide 17: Check: Pourbaix diagram
Calculate the dependency of potential on pH for the phase stability line governed by

## Slide 18: The very important O2 / H2O / H2 Pourbaix diagram
?
The line for O2(g) in the textbook is misplaced

## Slide 19: Exercises: O2 / H2O / H2 Pourbaix diagram
What are the lines?
Write reactions for the stability lines and derive the pH dependencies
Why are O3(g), H2O2, or OH* not represented?
Sketch lines with 0.6 V overpotential required to run the half cell reactions at any appreciable speed

## Slide 20: Working electrodes – materials and geometries
Active electrodes
vs
Inert electrodes
  Often catalytic
  Noble metals
  Graphite
  Glassy carbon
  Oxides
  Enzymes

## Slide 21: Check
What do the electrodes on the previous slide have in common? (According to the text book)
Discuss advantages and disadvantages to the different geometries
How can we eliminate or reduce gradients in the activities in reactants and products?
Name some active electrodes
For each of the examples of classes of inert electrodes, name an example and why it may be interesting

## Slide 22: Potentiometry
Measuring potentials at open circuit; thermodynamics
Connected to activities and concentrations via the Nernst equation
Measure vs suitable reference electrode
Ion-specific electrode, or ion-selective electrode (ISE)
Cu2+/ Cu and AgCl/Ag are examples of ISEs for Cu2+ and Cl- ions, respectively. But strong interference from e.g. Ag+ and Br- ions, respectively.

## Slide 23: Simple ISEs
Cu2+ / Cu
Cu2+(aq) + e- ↔ Cu(s)
AgCl / Ag
AgCl(s) + e- ↔ Ag(s) + Cl-(aq)
Cu
U
CuSO4(aq)
[Cu2+] = 1 M
Cu
[Cu2+] = ? M
Ag
KCl(aq)
[Cl-] = 1 M
Ag
[Cl-] = ? M
U
AgCl

## Slide 24: Solid electrolyte potentiometric sensors
pO2 sensor
“Lambda” sond
Zr0.9Y0.1O1.95
(YSZ)
O2-
vO**
U
pO2 = 0.21
pO2 = ?

## Slide 25: Solid electrolyte potentiometric sensors
pH2 sensor
Japanese TYK “NOTORP” for pH2 in molten aluminium based on proton conducting acceptor-doped CaZrO3
CaZr0.9Y0.1O2.95
(CZY)
H+
U
pH2 = 1 atm
pH2 = ?

## Slide 26: Ion-selective electrodes (ISEs)
We concentrate on one simple example; An ISE for F- ions.
The ISE is a AgCl/Ag electrode in KCl + KF solution with known [F-]inner
  The ISE membrane is selectively F- conductive
Reference is a AgCl/Ag electrode in KCl, open to test solution with unknown [F-]outer
  The reference membrane is open, e.g. a porous solid with a liquid junction inside
Everything is constant when [F-]outer changes, except membrane (Donnan) potential difference
Calibration necessary

## Slide 27: pH electrode
The pH electrode is an ISE where the membrane of the ISE is proton conducting
Glass exhibits a very small proton conductivity
Thin glass membrane offers sufficient proton conduction
  But the impedance of the pH electrode is still very high: noise and fluctuations

## Slide 28: Ch. 6 Summary
Activities:
Concentrations and partial pressures:
ISEs utilise potentials over ion selective membranes: